## Slide 1
INTRODUCTION
An industrially obtained consortium (IOC) of bacteria precipitates hazardous Pb(II) as PbS and Pb(0).
Dead bacteria has been widely studied as biomass for passive Pb(II) removal by adsorption (biosorption).
OBJECTIVE
Inhibit metabolic activity of IOC without damaging cell structure.
Investigate potential metabolically independent mechanism of Pb removal.
METHOD & MATERIALS
IOC grown in 20 g/L tryptone, 10 g/L yeast extract, 1 g/L NaCl, 0.041 g/L NaNO3 solution for 24 h.
IOC thereafter exposed to NaN3 for 3 h.
Dead IOC spiked in various amounts into different concentrations of Pb(II) .
Analytical methods: Aqueous Pb(II) measured with AA spectroscopy, metabolic activity measured with MTT, and surface characterized by FTIR spectroscopy.
RESULTS
Metabolic activity undetected after NaN3 sterilization.
Damage of cell structure undetected after NaN3 sterilization (Fig. 1b)
Fig. 1: FTIR spectra of IOC a) after 24 h growth period, b) after 3 h exposure to NaN3, and c) after exposure to NaN3 and Pb(NO3)2.
Pb(II) removal from solution corresponded with significant changes to cell structure (Fig. 1c), specifically observed as changes in amide, phosphate, and carboxyl groups.
61.7 % of 80 mg/L Pb(II) solution removed after 3 h by NaN3 sterilized IOC (Fig. 2).
Fig. 2: Percent lead remaining in solution as a function of time after the addition of the NaN3-sterilized consortium.
Maximum Pb(II) removal was observed at an initial concentration of 125 mg/L Pb(II) for IOC dosed between 25.2 and 47.5 mg/L..
Brandon van Veenhuyzen, Hendrik G. Brink, Evans M.N. Chirwa
deon.brink@up.ac.za
Microbial Pb(II) precipitation: the role of biosorption as a Pb(II) removal mechanism
University of Pretoria
Department of Chemical Engineering
Acknowledgements
National Research Foundation
CONCLUSIONS
Pb(II) removal not exclusive to living IOC.
Chemical binding of Pb(II) to cell surface plays a role in Pb(II) removal by dead IOC.
Dead IOC shows potential as an effective material for Pb(II) biosorption.